PPC Polyethylene Foam Self Adhesive Tapes

8300		Black  Linerless Medium/Firm PE Foam Tape

# DESCRIPTION

This versatile, fire resistant foam tape is used for a variety of sealing applications.

## FEATURES & BENEFITS

- Linerless construction for ease of use ‘on-site’ and to prevent unwinding or entanglement.

- Flexes to fill in and seal irregular surfaces.

- Powerful adhesive properties and high tack maintain positioning.

- Cushions and eliminates vibrations.

- Structure completely seals out air, moisture, light and dust when compressed by only 15% .

- Formulated from Polyethylene (PE) for high chemical and compression resistance.

- Insulates against temperature, sound and vibration.

- Resistant to many chemicals, acids and solvents.

## Technical Data

| ### Property |  |  | Test Method | Units | Data |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | 8300 |
| Density |  |  | ASTMD-1667 | Kg/m³ |  |  | 33 |
| Hardness |  |  | ASTMD-2240 | Shore 00 |  |  | 30 |
| Force to Compress 25% |  |  | ISO 844 | kPa |  |  | 35 |
| Compression Set 25% | After 5hrs |  | ISO 1856C | % change in height |  |  | 19 |
|  | After 24hrs |  |  |  |  |  | 10 |
| Water Absorption (7 days) |  |  | House | % of volume | <0.5 |  |  |
| Tensile Strength |  | Longways | ISO 1926 | kPa |  | 305 |  |
|  |  | Across |  |  |  | 205 |  |
| Percentage Elongation |  | Longways | ISO 1926 | % length |  | 150 |  |
|  |  | Across |  |  |  | 160 |  |
| Thermal Conductivity (K factor) |  | @10°C | ISO 2581 | w/mK | 0.030 |  |  |
|  |  | @40°C |  |  | 0.035 |  |  |
| Service Temperature |  |  | House | °C | -40 to 80 |  |  |
| Application Temperature |  |  | House | °C | 10-45 |  |  |
| Ring and Ball (Tack) |  |  | PSTC - 6 | °C | 104 |  |  |

NOTE

It is essential that this product be fully evaluated under the intended conditions before use. Changes in end-use conditions may require re-evaluation of the product under those conditions. Values quoted in this document are known typical values for this product and may vary. Please contact Precision Paper Coatings PTY LTD for any technical assistance.